Product Name:  Titanium silver grey  ZT7161

Appearance:  Grey powder.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No. Synthetic Fluorphlogopite          81-83             12003-38-2             77019

Titanium Oxide (TiO2)             17-18             13463-67-7             77891

Tin Oxide (SnO2)                   0-1              18282-10-5             77861

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range40-200µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           6.0-10.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     75-85 g oil/100g powder        GB 5211.15-88

Bulk Density:                       26-38 g/100cm3              GB/T 23771-2009

Density                            2.6-2.9 g / cm3 (water=1)