Product Name:  Titanium silver grey  ZT7111

Appearance:  Grey powder.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Fluorphlogopite         47-50              12003-38-2              77019

Titanium Oxide (TiO2)           48-50              13463-67-7             77891

Tin Oxide (SnO2)                 2-3               18282-10-5              77861

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range1-15µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.3 % max.                 GB 5211.3-85

Oil Absorption:                     50-70 g oil/100g powder        GB 5211.15-88

Bulk Density:                       17-21g/100cm3              GB/T 23771-2009

Density                            2.8-3.1g / cm3 (water=1)