Product Name:  Gold Luster Series ZT5310

Appearance:  A free flowing off gold powder with a bright luster.

Ingredients and Composition

Chemical Name               %               CAS No.         CI No.

Mica                    56-64             12001-26-2          77019

Titanium Oxide(TiO2)             15-19             13463-67-7          77891

Iron(III) Oxide(Fe2O3)            22-28              1309-37-1           77491

D50

Particle Size Distribution: 80% within the range10-60 µm.        (By Malvern Mastersizer2000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0 -11.0                   ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     70-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       15-30 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)