Product Name:  ZT2001

Appearance:   A free flowing off white powder with a bright golden reflection color.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Mica               53 -61             12003-38-2

Titanium Oxide(TiO2)            39-47              13463-67-7             77891

Tin Oxide (SnO2)                 <1                 18282-10-5             77861

Particle Size Distribution: 80% within the range10-60µm.        (By Malvern Mastersizer2000)

Visual and Colorimetric evaluation:    conforms                     KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                     ISO787-9

Loss on Drying(105℃):	0.5% max.                  GB 5211.3-85

Oil Absorption:                     50-90 g oil/100g powder         GB 5211.15-88

Bulk Density:                       10-40 g/100cm3               GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)