Product Name:  Exterior Red Kylin 96502WR

Appearance:  An red kylin, free flowing powder with a bright metal luster.

Ingredients and Composition

Chemical Name              %                CAS No.               CI No.

Synthetic Fluorphlogopite           53-58               12003-38-2

Iron(III) Oxide (Fe2O3)            37-42               1309-37-1               77491

Cerium Oxide (Ce2O3)                <1                1345-13-7                77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within（10-45）µm.          (By Malvern Mastersizer3000)

22.±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     45-75 g oil/100g powder        GB 5211.15

Bulk Density:                       20-45 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)