Product Name:  Exterior Pine Green 96234WR

Appearance:  A white, free flowing powder with a with a pine green reflection color.

Ingredients and Composition

Chemical Name               %                CAS No.              CI No.

Synthetic Fluorphlogopite           38-45              12003-38-2

Titanium Oxide (TiO2)             50-57              13463-67-7              77891

Cerium Oxide (Ce2O3)                <1                1345-13-7               77280

Tin Oxide (SnO2)             <1                18282-10-5              77861

Polymer                   1-5

D50

Particle Size Distribution: 90% within the range10-45µm.         (By Malvern Mastersizer2000)

20.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       40-60 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)