Product Name:  Exterior Dazzling Peacock Blue 96225WR

Appearance:  A white, free flowing powder with a bright blue reflection color.

Ingredients and Composition

Chemical Name              %                CAS No.              CI No.

Synthetic Fluorphlogopite         48-54              12003-38-2

Titanium Oxide (TiO2)           42-47               13463-67-7               77891

Cerium Oxide (Ce2O3)               <1                1345-13-7                77280

Tin Oxide (SnO2)            <1                18282-10-5               77861

Polymer                  1-5

D50

Particle Size Distribution: 90% within（10-45）µm.         (By Malvern Mastersizer3000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    GB 1717

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15

Bulk Density:                       20-45 g/100cm3              GB/T 23771

Density                            2.8-3.4 g / cm3 (water=1)