Product Name:  Exterior Penguin White 96103WR

Appearance:  A white color, free flowing powder with a pearl luster.

Ingredients and Composition

Chemical Name              %               CAS No.              CI No.

Synthetic Fluorphlogopite          68-74              12003-38-2

Titanium Oxide(TiO2)             21-27              13463-67-7               77891

Tin Oxide (SnO2)                     <1                18282-10-5               77861

Cerium Oxide (Ce2O3)                 <1                1345-13-7                77280

Silane Coupler KH-560             1-5                2530-83-8

D50

Particle Size Distribution: 90% within the range10-60µm.         (By Malvern Mastersizer2000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     70-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       20-40 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)