Product Name:  Exterior Royal Blue 92024WR

Appearance: An off-white, free flowing powder with an royal blue reflection color

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                   48-52             12001-26-2             77019

Titanium Oxide (TiO2)           46-50             13463-67-7             77891

Tin Oxide (SnO2)                 <1              18282-10-5             77861

Cerium Oxide (Ce2O3)               <1              1345-13-7              77280

Polymer                   1-5

D50

Particle Size Distribution: 90% within the range 8-40 µm.       (By Malvern Mastersizer2000)

18.0±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       20-40 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)