Product Name:  Tender silk gold  SW6311

Appearance:  Golden powder.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Mica                    15-28              12001-26-2             77019

Titanium Oxide (TiO2)             58-68              13463-67-7             77891

Tin Oxide (SnO2)                  ≤1                18282-10-5             77861

Diiron trioxide（Fe2O3）           14-16              1309-37-1              77491

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range1-15µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     50-65 g oil/100g powder        GB 5211.15-88

Bulk Density:                       38-45g/100cm3              GB/T 23771-2009

Density                            3.2-3.7g / cm3 (water=1)