Product Name:  Flash green gold   SW6315

Appearance:  Platinum Gold.

Ingredients and Composition

Chemical Name              %               CAS No.             CI No.

Synthetic Fluorphlogopite         46-67              12003-38-2             77019

Titanium Oxide (TiO2)            30-45              13463-67-7             77891

Tin dioxide (SnO2) 	≤2              18282-10-5             77861

Iron Oxide （Fe2O3）             3-7              1309-37-1              77491

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range30-150µm.        (By Malvern Mastersizer2000)

20.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           7.0-11.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     65-85g oil/100g powder        GB 5211.15-88

Bulk Density:                       32-45g/100cm3              GB/T 23771-2009

Density                            3.1-3.6g / cm3 (water=1)