Cosray Ray3D

MG5504-SF

INCI Name:    Mica,Iron Oxide, Black Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                    39.0-49.0%                                          CLRTM -51

Fe2O3                                                                        31.0-41.0%                                          CLRTM -48

Fe3O4                                                                                                15.0-25.0%                                         CLRTM -48

Odor:                                                                 Odorless                                                CLRTM -53

Particle Size:                                                      10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):              4.0-11.0                                               CLRTM-45

Oil Absorption:                                                 50.0-90.0g/100g                                   CLRTM -46

Density                                                                   2.7-3.6g/cm3                                           CLRTM -47

Microbiology:                                                  <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                      <1ppm

Sb                                                                       <2ppm

Cd                                                                      <5ppm

Zn                                                                      <100ppm

Ba                                                                      <50ppm

Cr                                                                       <100ppm

Cu                                                                      <50ppm

Ni                                                                       <200ppm