Cosray Diamond Orange

(Code: 8423R)

INCI Name:         Calcium Aluminum Borosilicate, Titanium Dioxide, Red 40 Lake, Tin Oxide

Chemical Composition:                                                                                               Test method

Calcium Aluminum Borosilicate                     64.0-83.0%                                             CLRTM-51

TiO2 (Rutile)                                                    12.0-20.0%                                             CLRTM -48

FD&C Red 40 Al Lake                                   5.0-15.0%                                              CLRTM -48

SnO2                                                                                     ≤1.0%                                             CLRTM -48

Appearance:                                              Orange Powder                                           CLRTM -52

Odor:                                                                Odorless                                                CLRTM -52

Particle Size:                                                   10-125μm                                               CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM -45

Oil Absorption:                                          50.0-95.0g/100g                                         CLRTM -46

Density                                                             2.5-3.5g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <20ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm