Cosray Crystal Lilac

(Code: 64301V)

INCI Name:          Synthetic fluorphlogopite, Titanium Dioxide, Manganese Violet, Tin Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                                        37.0-56.0%                                    CLRTM-51

TiO2 (Rutile)                                                         39.0-47.0%                                     CLRTM -48

Manganese Violet                                                 5.0-15.0%                                       CLRTM -48

SnO2                                                                     ≤1.0%                                             CLRTM -48

Appearance:                                                Violet Powder                                            CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                    10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-9.0                                                  CLRTM-45

Oil Absorption:                                             45.0-75.0g/100g                                     CLRTM -46

Density                                                               2.9-3.7g/cm3                                             CLRTM -47

Microbiology:                                                 <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                               CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm