Cosray Royal Blue

(Code: 4405B)

INCI Name:    Mica, Titanium Dioxide, Tin Oxide, Blue 1 Lake

Chemical Composition:                                                                                                Test method

Mica                                                                   33.0-51.0%                                           CLRTM-51

TiO2 (Rutile)                                                      44.0-52.0%                                           CLRTM -48

FD&C Blue 1 Al  Lake                                    5.0-15.0%                                              CLRTM -48

Appearance:                                                   Blue Powder                                          CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                 CLRTM-45

Oil Absorption:                                             60.0-100.0g/100g                                    CLRTM -46

Density                                                               2.4-3.1g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <10ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm