Cosray Rose-Red

(Code: 4204RV)

INCI Name: Mica, Titanium Dioxide,    Tin Oxide    Erythrosine, Amaranth

Chemical Composition:                                                                                              Test method

Mica                                                                   38.0-55.0%                                         CLRTM-51

TiO2 (Rutile)                                                      38.0-48.0%                                         CLRTM -48

Erythrosine Lake                                              4.0-8.0%                                            CLRTM -48

Amaranth Lake                                                 3.0-6.0%                                             CLRTM -48

SnO2                                                                  ≤ 1.0%                                             CLRTM -48

Appearance:                                              Rose-Red Powder                                      CLRTM -52

Odor:                                                                   Odorless                                           CLRTM -53

Particle Size:                                                     10-60μm                                             CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                CLRTM-45

Oil Absorption:                                             50.0-100.0g/100g                                   CLRTM -46

Density                                                               2.9-3.6g/cm3                                             CLRTM -47

Microbiology:                                                 <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                         <3ppm

Pb                                                                        <20ppm

Hg                                                                       <1ppm

Sb                                                                       <2ppm

Cd                                                                      <1ppm

Zn                                                                      <50ppm