Cosray Carbon

(Code: 4106SF)

INCI Name:                                         Mica, Titanium Dioxide, Tin Oxide, Black Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                   30.0-44.0%                                          CLRTM-51

TiO2 (Rutile)                                                      1.0-5.0%                                              CLRTM -48

Black Iron Oxide                                             55.0-65.0%                                           CLRTM -48

Appearance:                                             Blackish Green Powder                              CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                CLRTM-45

Oil Absorption:                                             55-100g/100g                                         CLRTM -46

Density                                                               2.9-3.6g/cm3                                             CLRTM -47

Microbiology:                                                 <100 cfu/g                                            CLRTM -54

No gram negative

Heavy Metals:                                                                                                               CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                      <1ppm

Sb                                                                       <2ppm

Cd                                                                      <5ppm

Zn                                                                      <100ppm

Ba                                                                      <50ppm

Cr                                                                       <100ppm

Cu                                                                      <50ppm

Ni                                                                       <200ppm