Cosray Crystal Flash Red Bronze

(Code: 6552C)

INCI Name:                                            Synthetic fluorphlogopite, Iron Oxide

Chemical Composition:                                                                                                Test method

Synthetic Mica                                            69.0-79.0 %                                               CLRTM-51

Fe2O3                                                            21.0-31.0%                                                CLRTM -48

Appearance:                                             Flash Red Bronze                                       CLRTM 52

Odor:                                                               Odorless                                                CLRTM -52

Particle Size:                                                  10-125μm                                               CLRTM -42

PH-Value (10% Aqueous Suspension):         4.0-11.0                                                 CLRTM -45

Oil Absorption:                                           45-95g/100g                                              CLRTM -46

Density                                                            2.6-3.3 g/cm3                                                CLRTM -47

Microbiology:                                                <100 cfu/g                                               CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                               <3ppm

Pb                                                               <10ppm

Hg                                                              <1ppm

Sb                                                              <2ppm

Ba                                                             <50ppm

Cd                                                             <1ppm

Cr                                                              <100ppm

Cu                                                             <50ppm

Ni                                                              <200ppm

Zn                                                             <50ppm