Cosray Satin White

(Code: 1007C)

INCI Name:                                                  Mica, Titanium Dioxide

Chemical Composition:                                                                                                       Test method

Mica                                                                       57.0-67.0%                                              CLRTM -51

TiO2 (Rutile)                                                         33.0-43.0%                                              CLRTM -48

Appearance:                                                        Silver white                                               CLRTM -52

Odor:                                                                     Odorless                                                  CLRTM -53

Particle Size:                                                         5-25μm                                                    CLRTM -42

Median size(D50):                                                7.0-17.0μm

pH-Value(10% Aqueous Suspension):             4.0-11.0                                                    CLRTM-45

Oil Absorption:                                                  50.0-90.0g/100g                                         CLRTM -46

Density                                                                2.8-3.3g/cm3                                              CLRTM -47

Microbiology:                                                    <100 cfu/g                                                  CLRTM -54

No gram negative

Heavy Metals:                                                                                                                        CLRTM -55

As                                                                          <3ppm

Pb                                                                         <10ppm

Hg                                                                        <1ppm

Sb                                                                         <2ppm

Cd                                                                        <1ppm

Zn                                                                        <50ppm