Cosray Super White

(Code: 1006C)

INCI Name:                                        Mica, Titanium Dioxide

Chemical Composition:                                                                                                       Test method

Mica                                                           66.0-76.0%                                                          CLRTM-51

TiO2                                                          24.0-34.0%                                                           CLRTM -48

Appearance:                                            Silver white                                                          CLRTM -52

Odor:                                                         Odorless                                                              CLRTM -53

Particle Size:                                             10-60μm                                                             CLRTM -42

pH-Value(10% Aqueous Suspension):   4.0-11.0                                                                CLRTM-45

Oil Absorption:                                       55.0-95.0g/100g                                                   CLRTM -46

Density                                                      2.7-3.2g/cm3                                                        CLRTM -47

Microbiology:                                          <100 cfu/g

No gram negative                                               CLRTM -54

Heavy Metals:                                                                                                                      CLRTM -55

As                                                                   <3ppm

Pb                                                                  <10ppm

Hg                                                                  <1ppm

Sb                                                                   <2ppm

Cd                                                                  <1ppm

Zn                                                                  <50ppm