Cosray Super Sparkle

(Code: 1002C)

INCI Name:                                           Mica,Titanium Dioxide,Tin Oxide

Chemical Composition:                                                                                                       Test method

Mica                                                          81.0-92.0%                                                          CLRTM -51

TiO2 (Rutile)                                            8.0-18.0%                                                              CLRTM -48

SnO2                                                          ≤1.0%                                                                 CLRTM -48

Appearance:                                            Silver white                                                          CLRTM -52

Odor:                                                       Odorless                                                                CLRTM-53

Particle Size:                                           40-200μm                                                              CLRTM -42

pH-Value(10% Aqueous Suspension):  4.0-11.0                                                                 CLRTM -45

Oil Absorption:                                 70.0-120.0g/100g                                                       CLRTM -46

Density                                                     2.6-3.0g/cm3                                                         CLRTM -47

Microbiology:                                         <100 cfu/g                                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                        CLRTM -55

As                                                                <3ppm

Pb                                                                <10ppm

Hg                                                               <1ppm

Sb                                                                <2ppm

Cd                                                               <1ppm

Zn                                                               <50ppm