Product Name:  Multi-Colour Series 2451S

Appearance:   A free flowing off white powder with a blue/green/gold multicolor effect.

Ingredients and Composition

Chemical Name               %             CAS No.             CI No.

Synthetic Fluorphlogopite          30-40            12003-38-2

Titanium Oxide(TiO2)            16-22            13463-67-7              77891

Tin Oxide (SnO2)                 <2              18282-10-5              77861

Cobalt(III) Oxide(Co2O3)             2-4             1308-04-9

Silicon Oxide (SiO2)           38-48              7631-86-9

D50

Particle Size Distribution: 80% within the range 10-45µm.        (By Malvern Mastersizer2000)

25.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           5.0 -8.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       30-60 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)