Cosray Yellow

(Code: 4102Y)

INCI Name:   Mica, Titanium Dioxide, Yellow Iron Oxide，Tin Oxide

Chemical Composition:                                                                                               Test method

Mica                                                                   32.0-51.0%                                         CLRTM-51

TiO2                                                                    44.0-52.0%                                         CLRTM -48

Yellow Iron Oxide                                            5.0-15.0%                                            CLRTM -48

SnO2                                                                       ≤1%                                              CLRTM -48

Appearance:                                                    Yellow Powder                                    CLRTM -52

Odor:                                                                   Odorless                                           CLRTM -53

Particle Size:                                                     10-60μm                                             CLRTM -42

pH-Value(10% Aqueous Suspension):             4.0-11.0                                              CLRTM-45

Oil Absorption:                                             50.0-90.0g/100g                                     CLRTM -46

Density                                                               2.9-3.6g/cm3                                             CLRTM -47

Microbiology:                                                 <100 cfu/g                                             CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                     <1ppm

Sb                                                                      <2ppm

Cd                                                                     <1ppm

Zn                                                                     <50ppm