Cosray Silver Black

(Code: 4602S)

INCI Name:     Mica, Titanium Dioxide, Black Iron Oxide

Chemical Composition:                                                                                                Test method

Mica                                                                        50.0-68.0%                                     CLRTM-51

TiO2 (Rutile)                                                           22.0-30.0%                                     CLRTM -48

Black Iron Oxide                                                  10.0-20.0%                                       CLRTM -48

Appearance:                                                   Silver Black                                           CLRTM -52

Odor:                                                                   Odorless                                            CLRTM -53

Particle Size:                                                     10-60μm                                              CLRTM -42

pH-Value(10% Aqueous Suspension):           4.0-11.0                                                CLRTM-45

Oil Absorption:                                             70.0-110.0g/100g                                   CLRTM -46

Density                                                               2.7-3.2g/cm3                                               CLRTM -47

Microbiology:                                                 <100 cfu/g                                              CLRTM -54

No gram negative

Heavy Metals:                                                                                                                CLRTM -55

As                                                                       <3ppm

Pb                                                                      <10ppm

Hg                                                                      <1ppm

Sb                                                                       <2ppm

Cd                                                                      <5ppm

Zn                                                                      <100ppm

Ba                                                                      <50ppm

Cr                                                                       <100ppm

Cu                                                                      <50ppm

Ni                                                                       <200ppm